Note:

This document contains information and notes in hidden text.

If you need assistance to view & hide text, instructions are at this link:

http://www.marlite.com/hidden-notes-instructions.aspx

Delete this note and hyperlink after editing is complete.

The following specification has been developed by

Marlite

202 Harger St.

Dover, Ohio 44622

Tel: (330) 343-6621 Fax: (330) 343-4668.

Email:  info@marlite.com  www.marlite.com

to assist Architects and Designers in the specification of Decorative Fiberglass Reinforced Plastic wall panel system for high wear areas.

Marlite Stamdard FRP Panels are excellent for sanitary environments since they facilitate washing and cleaning and do not support mold or mildew growth.  However, FRP panels are subject to the effects of continuous humidity and temperature.  Provide adequate ventilation for drying and do not use in high temperature areas.

Marlite Induro FRP provides an exceptionally wear resistant decorative panel; due to an exclusive process of thermally bonding melamine impregnated surfacing materials directly to the FRP core.  Designed to match or coordinate with popular High Pressure Laminates, these panels offer a superb array of decorative finishes and patterns from solid colors to wood-grains and abstract patterns.  Custom color and patterns are available upon request.

Marlite Artizan FRP panels offer a superb array of decorative printed rotogravure finishes with exceptional image integrity; unlimited varieties of woodgrain and abstract pattern plus tactile as well as visual textures.  Custom color and patterns are available upon request.

Marlite Envue Graphic FRP provides impressive visuals of high-resolution photographs, illustrations, logos, tile designs and custom graphics, all protected by Marlite’s tough Sani-Coat sealer. A special application process produces optimum graphic reproduction on a tough, sanitary surface.

Marlite Symmetrix with Sani-Coat FRP panels feature prefinished precision grid score lines that provide the look of tile without grout to clean or deteriorate.  Custom color and patterns are available upon request.

The section has been formatted in accordance with the principals embodied in the Construction Specifications  Institute's  Manual of Practice and is intended for use in conjunction with Contract Conditions, Bidding Conditions and General Requirements developed in accordance with CSI guidelines.

Notes to the specifier are included. Options that must be selected by the specifier are shown in brackets [         ].   Inapplicable clauses shall be deleted.

SECTION 09 7700 – FIBERGLASS REINFORCED WALL PANELS

GENERAL

SUMMARY

Section Includes:   Prefinished polyester glass reinforced plastic sheets and adhered to unfinished [gypsum] [cementitous] [untreated plywood] wallboard.

[Aluminum] [PVC] trim.

[PVC Wall base.]

Products Not Furnished or Installed under This Section:

Gypsum [Cementitious] substrate board.

Resilient Base.

RELATED SECTIONS

Section [____] – 	Gypsum [Cementitious] substrate board.

Section [____] - Wood [Metal] Stud Framing

Section [____] - Painting & Transparent Finishes.

Section [____] - Resilient Base.

REFERENCES

References are listed as a convenience and are often deleted in their entirety.  If required by the user agency delete references from the list below that are not actually required by the text of the edited section.

American Society for Testing and Materials:  Standard Specifications (ASTM)

ASTM D 256 -	Izod Impact Strengths (ft #/in)

ASTM D 570 -	Water Absorption (%)

ASTM D 638 -	Tensile Strengths (psi) & Tensile Modulus (psi)

ASTM D 790 -	Flexural Strengths (psi) & Flexural Modulus (psi)

ASTM D 2583- Barcol Hardness

ASTM D 5319 - Standard Specification for Glass-Fiber Reinforced Polyester Wall and Ceiling Panels.

ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

SUBMITTALS

Product Data:  Submit sufficient manufacturer's data to indicate compliance with these specifications, including:

Preparation instructions and recommendations.

Storage and handling requirements and recommendations.

Installation methods.

Shop Drawings:  Submit elevations of each wall showing location of paneling and trim members with respect to all discontinuities in the wall elevation.

Selection Samples:  Submit manufacturer’s standard color pattern selection samples representing manufacturer's full range of available colors and patterns.

Samples for Verification:   Submit appropriate section of panel for each finish selected indicating the color, texture, and pattern required.

Submit complete with specified applied finish.

For selected patterns show complete pattern repeat.

Exposed Molding and Trim:  Provide samples of each type, finish, and color.

Manufacturers Material Safety Data Sheets (MSDS) for adhesives, sealants and other pertinent materials prior to their delivery to the site (available as downloads for most Marlite’s products at http://www.marlite.com/tech-details.aspx or by contacting Marlite at info@marlite.com).

QUALITY ASSURANCE

Conform to building code requirements for interior finish for smoke and flame spread requirements as tested in accordance with:

ASTM E 84 (Method of test for surface burning characteristics of building Materials)

Wall Required Rating – Class [A] [C].

Include the following if products are used in areas subject to stringent wash down requirements.

### Sanitary Standards:  System components and finishes to comply with:

United States Department of Agriculture (USDA) / Food Safety & Inspection Services (FSIS) requirements for food preparation facilities, incidental contact.

#### Food and Drug Administration (FDA) 2013 Food Code 6-101.11.

Canadian Food Inspection Agency (CFIA) requirements.

DELIVERY, STORAGE AND HANDLING

Deliver materials factory packaged on strong pallets.

Store panels and trim lying flat, under cover and protected from the elements.  Allow panels to acclimate to room temperature (range of 60 to 75°F) for 48 hours prior to installation.

PROJECT CONDITIONS

Environmental Limitations:  Building are to be fully enclosed prior to installation with sufficient heat (70°) and ventilation consistent with good working conditions for finish work

During installation and for not less than 48 hours before, maintain an ambient temperature and relative humidity within limits required by type of adhesive used and recommendation of adhesive manufacturer.

Provide ventilation to disperse fumes during application of adhesive as recommended by the adhesive manufacturer.

WARRANTY

Furnish one-year guarantee against defects in material and workmanship.

PRODUCTS

ACCEPTABLE MANUFACTURER

Marlite;   1 Marlite Drive, Dover, OH  44622.  800-377-1221 FAX (330) 343-4668 Email:  info@marlite.com www.marlite.com.

Product:

Standard FRP

Laminated FRP

PANELS

Fiberglass reinforced thermosetting polyester resin panel sheets complying with ASTM D 5319.

Dimensions:

Thickness – 0.090 “ (2.29mm) nominal

Width - 4'-0”  (1.22m) nominal

Induro FRP Panels are not available in lengths exceeding 8’ (2.4m).

Length – [10’-0” (3.0m)][8’-0” (2.4m) ][As indicated on the drawings] nominal

Tolerance:

Length and Width:  +/-1/8 “ (3.175mm)

Square -  Not to exceed 1/8 “ for 8 foot (2.4m) panels or 5/32 “ (3.96mm) for 10 foot (2.4m) panels

Properties:  Resistant to rot, corrosion, staining, denting, peeling, and splintering.

Flexural Strength - 1.7 x 104 psi per ASTM D 790.

Flexural Modulus – 6.0 x 105 psi per ASTM D 790.

Tensile Strength – 8.0 x 103 psi per ASTM D 638.

Tensile Modulus – 9.43 x 105 psi per ASTM D 638.

Water Absorption - 0.17% per ASTM D 570.

Barcol Hardness (scratch resistance) of 30 as per ASTM D 2583.

Izod Impact Strength of 7.0 ft. lbs./in ASTM D 256

Back Surface:  Smooth.  Imperfections which do not affect functional properties are not cause for rejection.

Select finish from our full Marlite Finish Palette at www.marlite.com or contact Marlite to create your own finish.

Front Finish: [As Indicated on the Drawings] [In accordance with preapproved sample.  Information available from the Architect’s Office][ __________________________________}

Specifier Note: Marlite’s Standard FRP panels are available in several configurations, including Class A (I) and Class C (III) Fire-rated, along with various surface textures – smooth and pebble.   Color: [Specifier to choose.]

Marlite Standard FRP is available in a variety of colors, including;

P100 White

P106 Beige

P118 Natural Almond

P140 Ivory

P145 Silver

P151 Light Grey

P807 Black

P199 Bright White

P400N Red

P410N Brown

P420N Blue

P430N Medium Grey

P440N Biscuit

P450N Maroon

P460N Light Yellow

P470N Dark Grey

S100 S/2/S White

S100G White

S118G Almond

S490N S2S Light Grey

S807N Black

Custom patterns and colors are available.  Minimum quantities may apply.  Contact a Marlite representative for details.

        - Surface [Specifier to choose.] Marlite Standard FRP and Symmetrics are available on two standard surface textures. Pebbled (indicated by “P” designation i.e., P 100 White) and Smooth (indicated by “S” designation i.e., S 100 White).

        - Fire Rating [Specifier to choose.] Marlite FRP is available in either Class A (I) or Class C (III) Fire Rating.  Specifier should add designation to product number only for Class A (i.e., P 100 White, Class A).

        - Size: [Specifier to choose, or as indicated on drawings.] standard sizes are;

          - Marlite Standard FRP

            - 48” x 96” [1.2m x 2.4m] x .090” (3mm) nom.

            - 48” x 108” [1.2m x 2.7m] x .090” (3mm) nom.

            - 48” x 120” [1.2m x 3m] x .090” (3mm) nom.

          - Ceiling panels (designed for suspended ceiling installation)

- 23 ¾” x 47 ¾” (0.6m x 1.2m) x  .090” (3mm)

- 23 ¾” x 23 ¾” (0.6m x 0.6m) x  .090” (3mm)

Can be specified as FRP panels only or backed with 5/8” FR Drywall.

          - Laminated FRP

- 48” x 96” [1.2m x 2.4m] x .090” (3mm) nom.

Delete the following if resilient or contractor supplied bases are used.

BASE

Marlite Base Molding for 0.090” (2.29mm) thick FRP Panels

Color: [Black] [Quarry Red].

Profiles:

M 612 FRP Base Molding, 10’ length

M 651 Inside Corner

M 660 Outside Corner

M 620 LH End Cap

M 625 RH End Cap

MOLDINGS

Select PVC or Aluminum trims. A

Aluminum Anodized Trim:  Heavy weight extruded aluminum 6063-T5 alloy prefinished at the factory.

Profiles	:

The following are extruded aluminum trim profiles.

F 550 Inside Corner, 8’ length

F 561 Outside Corner, 8’ length

F 565 Division, 8’ length

F 570 Edge, 8’ length

Color: [Brite Satin Anodized][Black Satin Anodized]

The following are extruded aluminum trim profiles.

The following are extruded PVC trim profiles. PVC colors are also available to coordinate with Sani-Coat colorways.  See current Marlite Finish Guide for available choice.

PVC Trim:  Thin-wall semi-rigid extruded PVC.

M 350 Inside Corner, [8’ length][10’ length]

M 360 Outside Corner, [8’ length][10’ length]

M 365 Division, [8’ length][10’ length]

M 370 Edge, [8’ length][10’ length]

V 177 135° Inside Corner [8’ length] [White only]

V 179 135° Outside Corner [8’ length] [White only]

Color:  [White][Beige][Natural Almond][Ivory][Silver][Light Grey][Black]

The following are dual-durometer extruded polypropylene trim profiles with Marlite’s exclusive Dual-Seal Technology, designed to restrict the growth and propagation of harmful pathogens. Standard colorways are extruded with color throughout the profile.

Outside Corner Guard:

F 560SS Stainless Corner Guard, [8’ length][10’ length]

Finish:  #4 brushed satin

M 961 PVC Outside Corner Guard

Color: [White, [8’ length][10’ length]][Natural Almond, [8’ length][10’ length]][Ivory, 10’ length][Silver, 10’ length][Light Grey, 10’ length]

ACCESSORIES

Specify rivets for use in areas with dramatic changes in temperature and/or humidity, where the substrate is unusually uneven, and in all low temperatures or cold storage applications.

Fasteners:  Non-staining nylon drive rivets.

Match panel colors.

Length to suit project conditions.

Adhesive:  Either of the following construction adhesives complying with ASTM C 557.

Marlite C-551 FRP Adhesive - Water- resistant, non-flammable adhesive.

Marlite C-915 Construction Adhesive - Flexible, water-resistant, solvent based adhesive, formulated for fast, easy application.

Titebond Advanced Polymer Panel Adhesive – VOC compliant, non-flammable, environmentally safe adhesive.

Sealant:

Marlite Brand MS-250 Clear Silicone Sealant.

Marlite Brand MS-251 White Silicone Sealant.

Marlite Brand - Color Match Sealant.

EXECUTION

PREPARATION

Examine backup surfaces to determine that corners are plumb and straight, surfaces are smooth, uniform, clean and free from foreign matter, nails countersunk, joints and cracks filled flush and smooth with the adjoining surface.

Verify that stud spacing does not exceed 24” (61cm) on-center.

Repair defects prior to installation.

Level wall surfaces to panel manufacturer’s requirements.  Remove protrusions and fill indentations.

INSTALLATION

Comply with manufacturer's recommended procedures and installation sequence.

Cut sheets to meet supports allowing 1/8” (3 mm) clearance for every 8 foot (2.4m) of panel.

Cut and drill with carbide tipped saw blades or drill bits, or cut with shears.

Pre-drill fastener holes 1/8” (3mm) oversize with high speed drill bit.

Space at 8” (200mm) maximum on center at perimeter, approximately 1” from panel edge.

Space at in field in rows 16’ (40.64cm) on center, with fasteners spaced at 12” (30.48 cm) maximum on center.

Apply panels to board substrate, above base, vertically oriented with seams plumb and pattern aligned with adjoining panels.

Install panels with manufacturer's recommended gap for panel field and corner joints.

Adhesive trowel and application method to conform to adhesive manufacturer’s recommendations.

Drive fasteners for snug fit.  Do not over-tighten.

Apply panel moldings to all panel edges using silicone sealant providing for required clearances.

All moldings must provide for a minimum 1/8 “(3mm) of panel expansion at joints and edges, to insure proper installation.

Apply sealant to all moldings, channels and joints between the system and different materials to assure watertight installation.

CLEANING

Remove excess sealant from panels and moldings.  Wipe panel down using a damp cloth and mild soap solution or cleaner.

Refer to manufacturer's specific cleaning recommendations Do not use abrasive cleaners.

END OF SECTION 09 7700